## Slide 1
Probabilistic Assessment of VVER-440 reactor pressure vessel subjected to pressurized thermal shocks
Vladislav Pištora, Katarína Šišková, Miroslav Pošta
ÚJV Řež, a. s.
3rd International Seminar on Probabilistic Methodologies for Nuclear Applications (ISPMNA)
October 22-24,2019, Rockville, MD, USA

## Slide 2: OUTLINES
VVER-440 reactor pressure vessel
Scheme of RPV integrity assessment
Applicable standards for VVER
Main parts of probabilistic RPV integrity assessment
Main parameters entering probabilistic assessment as statistical distributions
  Randomly generated cracks
  Fracture toughness
Establishing the conditional probability of fast fracture initiation
Acceptance criteria
Probabilistic assessment of pressurised thermal shocks for VVER 440 reactor pressure vessel

## Slide 3: VVER-440 reactor pressure vessel
VVER 440 – water cooled water moderated energy reactor
Similar to PWR
Originally designed in Soviet Union in 70s
Electrical power 440 MW (design)
Beltline inner radius 1,771 m
Wall thickness in beltline 140 mm (base mat.) + 9 mm (cladding)
Maximum design fluence for 40 years: 323.1022 m-2 (neutrons with energy > 0,5 MeV)
Design fluence for 40 years at weld No. 5/6: 248.1022 m-2
Base material in beltline 15Kh2MFA
Weld material 10KhMFT
weld 3/5
weld 5/6
long ring
upper short ring
lower nozzle ring
Region entering probabilistic PTS

## Slide 4: General scheme of deterministic RPV integrity assessment
3

## Slide 5: General scheme of probabilistic RPV integrity assessment
4

## Slide 6: Probabilistic PTS analyses
Some input parameters are taken as stochastic, described by distributions.
Using probabilistic methods (e.g. simulations), the risk is quantitatively evaluated (it is usually non-zero).
The result is expressed in terms of frequency of brittle fracture initiation or frequency of RPV failure.
Criterion for acceptable risk is given by regulatory authority.

## Slide 7: Probabilistic vs. deterministic PTS analyses
Deterministic parts in probabilistic PTS analyses:
  all mathematical models used within the PTS analyses
  all input data for thermal hydraulic calculations (and thus also output data from thermal hydraulic analyses)
  RPV dimensions
  thermal and tensile properties of RPV material
Probabilistic parts in deterministic analyses:
Current deterministic PTS analyses include many input parameters only at some probabilistic level or including additional safety margin (not real „100%“ lower/upper bound), e.g.:
  fracture toughness curve (KIC)
  transition temperature shift prediction
  fluence
  postulated crack: in RPV wall, non-existence of a crack larger than the postulated one is assured only with some probability (lower than 100%)
  events with very low frequency of occurrence are not considered (are „screened“)

## Slide 8: Example of stochastic data
Chart: T - T0, °C
B=16 | 37.8885 | 34.3108 | 30.7331 | 45.044 | 43.2551 | 48.6217 | 44.1495 | 47.7272 | 52.1994 | 56.6715 | 52.1994 | 58.4604 | 54.8827 | 59.3548 | 32.522 | 43.2551 | 33.4164 | 42.3607 | 59.3548 | 60.2492 | 78.1378 | 58.4604 | 62.9325 | 75.4545 | 70.0879 | 84.3988 | 127.3313 | 43.2551 | 61.1437 | 53.9882 | 76.3489 | 70.9823 | 87.9765
B=30 | 51.3991 | 69.1919 | 104.7774 | 112.1039 | 98.4976
B=37.5/40 | 64.2673 | 85.2942 | 131.7749 | 106.3212 | 137.3083 | 105.4759 | 134.7176 | 145.9645 | 185.3283 | 221.3182 | 41.369 | 54.8652 | 42.4937 | 57.1145 | 67.2367 | 84.1069 | 123.061 | 115.2194
B=75 | 104.2287 | 112.1252 | 125.2859 | 151.6074 | 146.3431 | 184.5093 | 158.1878 | 259.5255 | 318.7488 | 413.5061 | 416.1383 | 322.697 | 214.779 | 321.3809 | 270.0541 | 389.8168 | 381.9204
B=100 | 97.7817 | 118.9949 | 120.4092 | 107.6812 | 126.066 | 121.8234 | 124.6518 | 130.3087 | 147.2792 | 137.3797 | 158.5929 | 175.5635 | 38.3848 | 48.2843 | 61.0122 | 68.0833 | 118.9949 | 94.9533 | 161.4214 | 56.7696 | 52.5269 | 53.9411 | 62.4264 | 116.1665 | 48.2843 | 75.1543 | 80.8112 | 92.1249 | 118.9949 | 126.066 | 127.4802 | 38.3848 | 36.9706 | 45.4558 | 66.669 | 99.196 | 169.9066 | 100.6102 | 297.1859 | 335.3696 | 267.4874 | 285.8721 | 287.2864 | 305.6711 | 273.1442 | 181.2203 | 205.262 | 459.8204 | 233.5462 | 423.0509 | 365.0681 | 179.8061 | 362.2397 | 373.5534 | 365.0681
B=125 | 133.6465 | 187.4791 | 169.5349 | 127.6651
B=150 | 199.9847 | 235.9817 | 223.461 | 226.5912 | 290.7596 | 192.1593 | 265.7183 | 304.8454 | 293.8898 | 303.2803 | 323.6264 | 142.0766 | 159.2925 | 273.5437 | 207.8101 | 225.0261 | 267.2834 | 320.4962 | 306.4105 | 212.5054 | 248.5023 | 257.8929 | 286.0644 | 276.6739 | 251.6325 | 276.6739 | 267.2834 | 181.2037 | 184.3339 | 210.9403 | 257.8929 | 217 | 220.3308 | 223.461 | 370.5789 | 231.2864
KCJ(mean) | 34.0491 | 34.8964 | 35.9209 | 37.1599 | 38.6581 | 40.4698 | 42.6606 | 45.3098 | 48.5134 | 52.3873 | 57.0719 | 62.7366 | 69.5868 | 77.8703 | 87.8871 | 100 | 114.6475 | 132.3599 | 153.7787 | 179.6793 | 210.9997 | 248.8738 | 294.673 | 350.0558 | 417.0273 | 498.0126 | 595.9441 | 714.3676 | 857.5713 | 1030.7402 | 1240.1447
KCJ(5%) | 27.5865 | 28.044 | 28.5973 | 29.2663 | 30.0754 | 31.0537 | 32.2367 | 33.6673 | 35.3972 | 37.4892 | 40.0188 | 43.0778 | 46.7769 | 51.25 | 56.6591 | 63.2 | 71.1096 | 80.6744 | 92.2405 | 106.2268 | 123.1398 | 143.5918 | 168.3234 | 198.2301 | 234.3947 | 278.1268 | 331.0098 | 394.9585 | 472.2885 | 565.7997 | 678.8782
Temperature dependence of static fracture toughness of WWER-440 RPV materials adjusted to 1T assessed by Master Curve approach

## Slide 9: Applicable standard for VVER – VERLIFE / NTD ASI
Requirements for VVER RPV specific probabilistic integrity assessment are given in „Guidelines for Integrity and Lifetime Assessment of Components and Piping in WWER Nuclear Power Plants (IAEA – NULIFE - VERLIFE)“.
The detailed procedure is given in its Appendix XVI, the criteria are given in the main document.
VERLIFE is focussed on VVER reactors. Most of the procedure can be applied to other PWRs.
The Czech translation of IAEA – NULIFE – VERLIFE guidelines, issued as the „Normative Technical Documentation of the Association of Mechanical Engineers“, was accepted by the Czech regulatory body – SÚJB.

## Slide 10: Applicable standard for VVER – VERLIFE / NTD ASI
Generally, the VERLIFE procedure follows the approach developed in the USA, namely as described in NUREG-1806.
Main differences:
RTNDT is not applicable to VVERs. The whole fracture mechanical assessment is based directly on Master curve approach with transition temperature T0. (For some VVERs, fracture toughness specimens for establishing T0 are included in surveillance programme.)
No axial welds in VVER RPVs.
Underclad cracks considered.

## Slide 11: Stages of probabilistic assessment
  1) PSA (Probabilistic Safety Assessment) – PTS-specific PSA for probabilistic RPV integrity assessment
  Development of event trees for all possible PTS transients.
  Grouping of the events into groups („bins“) with similar course.
  Selection of a representative transient in each group (transient with the most adverse course form the RPV integrity point of view in the group).
  Determination of the frequency of occurrence of individual events in the group and (as the sum) the frequency of occurrence of the group.
  2) Determination of conditional probability of fast fracture initiation for all selected representative PTS transients.
  If crack arrest is taken into account, conditional probability of RPV failure is determined.
  Monte Carlo method is recommended: individual values of parameters are repeatedly randomly sampled from given statistical distributions – random RPVs and random flaws in them are generated. For the whole set of randomly sampled parameters, the „deterministic“ assessment of RPV integrity is performed.

## Slide 12: Probabilistic evaluation (simplified scheme)

## Slide 13: Deterministic part of the assessment
Thermal hydraulic analyses
  system thermal hydraulic analyses
  detailed mixing analyses
  as a simplified approach, it is possible to perform the system thermal hydraulic analyses only, i.e. not taking into account cold plumes
Calculations of temperature and stress fields
FEM calculations with using one-dimensional axisymmetric elements may be performed
Calculations of stress intensity factor KI
It is sufficient to use analytical methods based on stresses calculated on models without crack

## Slide 14: Establishing the conditional probabilities of fast fracture initiation, CPIjl

## Slide 15: Main parameters entering probabilistic assessment as statistical distributions
Neutron fluence – normal distribution
Chemical composition of RPV materials (Cu, P content) – normal distribution, applied only in some cases
Initial value of MC reference temperature T0 – normal distribution, standard deviation prescribed
Reference temperature shift ΔT0 - determined in dependence on neutron fluence and chemical composition according to formulae from VERLIFE, with normal distribution or based on Surveillance specimens programmes results
Randomly generated cracks (see below)
Fracture toughness (see below)

## Slide 16: Randomly generated cracks
Types of cracks entering the evaluation (VVER according to VERLIFE)
  Underclad cracks (in base metal, positioned precisely under the cladding, axial orientation only, semi-elliptical or elliptical) – not considered in the USA
  Embedded cracks in the weld (circumferential orientation only, elliptical)
  Embedded cracks in base metal (50 % circumferential, 50 % axial, elliptical)

## Slide 17: Randomly generated cracks
Statistical distributions are to be derived from statistical treatment of data obtained for flaws detected in the evaluated RPV. These data may be obtained from manufacturing, pre-operational or in-service inspections.
The types of statistical distributions for the following crack parameters are only the recommended ones:
  Crack density (number of cracks in a particular volume of material) - Poisson distribution
  Crack depth - exponential distribution
  Crack shape (semi-axes ratio or semi-axes difference) - exponential distribution
  Flaw location in RPV (distribution of embedded cracks along RPV wall thickness) - uniform distribution
  The relevant parameters of Poisson or exponential distributions are treated also as random values with gamma distribution.

## Slide 18: Randomly generated cracks
Complementary distribution function of exponential distribution of flaws
y =e
-0.7679(x-1.9147)
0
0,1
0,2
0,3
0,4
0,5
0,6
0,7
0,8
0,9
1
1,1
0
1
2
3
4
5
6
7
8
9
10
D (relative crack depth) [% wall thickness]
P(X>D)
Flaws in weld
Example of statistical treatment of embedded flaws in weld

## Slide 19: Randomly generated cracks
Example of statistical treatment of subcladding flaws
Complementary distribution function of exponential distribution of flaws
y = e
-1.4773(x-1.88164)
0
0,1
0,2
0,3
0,4
0,5
0,6
0,7
0,8
0,9
1
1,1
0
1
2
3
4
5
D (relative crack depth) [% wall thickness]
P(X>D)
subcladding flaws

## Slide 20: Fracture toughness
Statistical distribution of fracture toughness values is assumed to be the Weibull distribution, in accord with the Master Curve concept. Median of fracture toughness values (for specimens of thickness 1 inch = 25,4 mm) is assumed
KJc(med) = 30 + 70 exp[0.019(T-T0)]
Master Curve concept application: for a randomly generated reference temperature T0 and actual temperature of material T (dependent on time τ of the running PTS), value of Weibull distribution parameter K0 is determined:
K0() = 20 + [11 + 77 exp(0,019(T()-T0))][25/L]1/4
(correction on crack length L is considered)

## Slide 21: Fracture toughness

## Slide 22: Fracture toughness (distribution function)
Chart: Probability of fracture, T = T0

## Slide 23: Conditional probability of fast fracture initiation
Conditional probability of fast fracture initiation for time  is determined (for crack k, vessel l and scenario j) directly from the formula:
where Kmin = 20 MPa.m1/2
Note: Fracture toughness values need not be randomly generated within this particular part of the evaluation (as are the other stochastic quantities entering the evaluation) and adequately, the probability of fracture need not be determined through the Monte Carlo method, but the „cpi“ may be directly calculated according to Master Curve concept, using the above presented formula.

## Slide 24: Final probabilistic assessment
Conditional probability of fast fracture initiation over the entire PTS event for j-th scenario, l-th vessel and m-th crack is determined as its maximum over the time interval:
Determination of total conditional probability of fast fracture initiation CPIjl: for j-th scenario and l-th vessel with the set of m randomly generated cracks, the following relation is used
Determination of (unconditional) frequency of occurrence of fast fracture initiation for the l-th simulated vessel (for the whole set of PTS scenarios)
(summation over scenarios j, frequencies frj are also stochastic)

## Slide 25: Final probabilistic assessment - acceptance criteria
For the final evaluation, the mean value and the 95% percentile FI95% of (unconditional) frequency of occurrence of fast fracture initiation is used. This value is calculated over all simulated vessels.
In case that probabilistic evaluation of RPV resistance is performed based on frequency of initiation of fast fracture FI the following relation is used as an acceptance criterion:
and
The same conditions are used for frequency of RPV failure FF.
In the previous version of VERLIFE and NTD ASI, the criterion was
24
.

## Slide 26: Probabilistic assessment of pressurised thermal shocks for VVER 440 reactor pressure vessel
A PTS-specific PSA (PSA focussed on PTS) was performed. The current “classical” PSA model, focussed on core damage, was used as a basis, but it had to be significantly modified, as events leading to PTS have in most cases opposite character than those leading to core damage.
Finally, 44 groups of events were selected. The events were of the following types: LOCA, main steam line break, primary-to-secondary leak, and others.
The mean frequencies of occurrence frj of the groups were in the range 10-2 to 10-6 (groups with frj < 5.10-6 were screened).
Each of the groups was "covered" by a representative scenario analysed by system thermal hydraulic code RELAP5 (most of them were analysed previously, in the frame of deterministic PTS analyses).
25

## Slide 27: Probabilistic assessment of pressurised thermal shocks for VVER 440 reactor pressure vessel
For probabilistic fracture mechanics analyses the PROVER software package developed in UJV Rez (on the basis of US FAVOR code) was used.
PROVER software (similarly to FAVOR) consists of 3 codes:
    VERLOAD (calculations of temperature and stress fields),
    VERPFM (probabilistic fracture mechanics – establishing CPI),
    VERPOST (final assessment – combining frequencies of groups and CPI)
For the analyses, 200000 simulations of RPV were used. The typical resulting mean value of CPI for significant PTS representative scenarios was in the range 10-7 to 10-9/reactoryear.
26

## Slide 28: Probabilistic assessment of pressurised thermal shocks for VVER 440 reactor pressure vessel - results
27

## Slide 29: Probabilistic assessment of pressurised thermal shocks for VVER 440 reactor pressure vessel - results
Dominating contributors to FI – groups: PTS with flooding of RPV from outside: break of feedwater, small-break LOCA.
Dominating contributors to FI - individual types of defects: circumferential cracks in welds.
28

## Slide 30: Re-assessment
29
Original probabilistic RPV integrity assessment was performed in 2014.
After 5 years, the re-assessment is ongoing (finished at the end of 2019) with these new features:
  new PSA (slightly modified groups, re-assessed frequencies),
  new thermal hydraulic analyses (for some representative scenarios),
  new neutron fluences,
  new embrittlement trend curves (based on surveillance specimens),
  new acceptance criteria.

## Slide 31: SUMMARY - steps of probabilistic RPV integrity assessment
Perform PTS-specific PSA with the following results:
  Selection of groups of PTS scenarios.
  Establishing frequency of occurrence of each group (as statistical distribution).
  Selection of a representative PTS transient in each group.
For each representative PTS transient perform (deterministic):
  Thermal hydraulic analysis.
  Calculations of temperature and stress fields.
  Calculations of stress intensity factor KI.

## Slide 32: SUMMARY - steps of probabilistic RPV integrity assessment
Determine the following input data as statistical distributions:
  Neutron fluence
  Chemical composition (if necessary)
  Initial value of MC reference temperature T0
  Reference temperature shift ΔT0
  Randomly generated cracks
  Fracture toughness (given by standard)
Using the Monte Carlo method, calculate the conditional probability of fast fracture initiation (or conditional probability of RPV failure) for each PTS.
Determine the unconditional frequency of occurrence of RPV fast fracture initiation (or RPV failure).
Compare it with the acceptance criteria given by the standard.

## Slide 33
Thank you for your attention
32
Notes: [PLACEHOLDER TEXT]