## Slide 1: STATISTICAL CHARACTERIZATION OF CANDU PRESSURE TUBE INNER DIAMETER AND WALL THICKNESS USING ULTRASONIC INSPECTION DATA FOR PERFORMING FITNESS FOR SERVICE EVALUATIONS
Suresh Datla, Dirk Leemans, Jaff Robertson, Kinectrics Inc.
3rd International Seminar on Probabilistic Methodologies for Nuclear Applications
October 22-24, 2019
Rockville, MD, USA

## Slide 2: Outline
Introduction - Relevance of pressure tube dimensions in the demonstration of fitness for service (FFS) in CANDU fuel channels
Modelling - Current approaches taken to modelling pressure tube internal diameter and wall thickness
Characterizing the uncertainty of these dimensional models
Example use of CSA N285.8 Annex G to perform an uncertainty analysis of these dimensional models
Conclusions

## Slide 3: Introduction
Individual Zr-2.5Nb pressure tubes (380 to 480) passing horizontally through the reactor core.
Operation
  Internal Pressure (~10MPa)
  Temperature (2500C-3100C)
  Fast Neutron Fluxes
  (~1017 neutrons/m2/s)
PT Dimensions
  Creep/growth
  Corrosion/Wear
Accurate Characterization
of PT dimensions
to demonstrate FFS
CANDU Pressure Tubes (PT)
Ref: Above image is from CANTEACH image library. https://canteach.candu.org/Pages/ImageLibrary.aspx:

## Slide 4: Introduction
CANDU Pressure Tubes (PT)
Ref: Above image is from CANTEACH image library. https://canteach.candu.org/Pages/ImageLibrary.aspx:

## Slide 5: Fitness-for-Service (FFS) Assessments – PTID/WT
Pressure Tube Inner Diameter (PTID) and Wall Thickness (PTWT) for FFS applications
Design Rates
  Design creep strain and design corrosion and wear allowances
PTID/WT Modelling
  Simplified models derived from deformation equation in the literature
  Regression model based on in-service data
  Axial profile over the entire length of the pressure tube

## Slide 6: Inspections
Example of PTID profile scan along with extraction points for a particular channel
Chart: Axial Location (mm)
Extract-Mean | 103.99 | 104.58 | 104.96 | 105.55 | 105.8 | 105.99 | 106.23 | 106.33 | 106.38 | 106.41 | 106.45 | 106.44 | 106.37 | 106.38 | 106.36 | 106.29 | 106.27 | 106.23 | 106.11 | 106.07 | 106.01 | 105.9 | 105.87 | 105.8 | 105.65 | 105.6 | 105.53 | 105.4 | 105.34 | 105.25 | 105.09 | 105.02 | 104.93 | 104.72 | 104.64 | 104.52 | 104.26 | 104.12 | 104.02
Extract-Max | 104.05 | 104.61 | 105 | 105.6 | 105.85 | 106.04 | 106.29 | 106.37 | 106.42 | 106.5 | 106.5 | 106.48 | 106.43 | 106.44 | 106.43 | 106.38 | 106.34 | 106.28 | 106.17 | 106.1 | 106.06 | 106.04 | 105.92 | 105.86 | 105.69 | 105.66 | 105.58 | 105.44 | 105.48 | 105.32 | 105.15 | 105.08 | 104.98 | 104.77 | 104.69 | 104.56 | 104.32 | 104.2 | 104.11
Extract-Min | 103.93 | 104.55 | 104.94 | 105.52 | 105.77 | 105.95 | 106.2 | 106.3 | 106.34 | 106.34 | 106.39 | 106.39 | 106.31 | 106.32 | 106.3 | 106.2 | 106.23 | 106.17 | 106.06 | 106.01 | 105.97 | 105.76 | 105.82 | 105.77 | 105.63 | 105.55 | 105.48 | 105.32 | 105.19 | 105.18 | 105.05 | 104.97 | 104.87 | 104.69 | 104.59 | 104.47 | 104.19 | 104.02 | 103.9

## Slide 7: Inspections
CSA N285.4, “Periodic inspection of CANDU nuclear power plant components”
Source of the data is the filtered dump file that is created for every full length dimensional inspection channel.
  max/mean/min PTID and max/mean/min PTWT for every ~2mm of each tube
A script identifies the bundle constriction locations (12 or 13).
3 data points per bundle are selected (i.e. equally spaced within the bundle constrictions locations).
Ultrasonic Inspection Data

## Slide 8: Inspections
Example of PTID profile scan to show bundle constrictions
Chart: Axial Location (mm)
Extract-Mean | 103.99 | 104.58 | 104.96 | 105.55 | 105.8 | 105.99 | 106.23 | 106.33 | 106.38 | 106.41 | 106.45 | 106.44 | 106.37 | 106.38 | 106.36 | 106.29 | 106.27 | 106.23 | 106.11 | 106.07 | 106.01 | 105.9 | 105.87 | 105.8 | 105.65 | 105.6 | 105.53 | 105.4 | 105.34 | 105.25 | 105.09 | 105.02 | 104.93 | 104.72 | 104.64 | 104.52 | 104.26 | 104.12 | 104.02
Extract-Max | 104.05 | 104.61 | 105 | 105.6 | 105.85 | 106.04 | 106.29 | 106.37 | 106.42 | 106.5 | 106.5 | 106.48 | 106.43 | 106.44 | 106.43 | 106.38 | 106.34 | 106.28 | 106.17 | 106.1 | 106.06 | 106.04 | 105.92 | 105.86 | 105.69 | 105.66 | 105.58 | 105.44 | 105.48 | 105.32 | 105.15 | 105.08 | 104.98 | 104.77 | 104.69 | 104.56 | 104.32 | 104.2 | 104.11
Extract-Min | 103.93 | 104.55 | 104.94 | 105.52 | 105.77 | 105.95 | 106.2 | 106.3 | 106.34 | 106.34 | 106.39 | 106.39 | 106.31 | 106.32 | 106.3 | 106.2 | 106.23 | 106.17 | 106.06 | 106.01 | 105.97 | 105.76 | 105.82 | 105.77 | 105.63 | 105.55 | 105.48 | 105.32 | 105.19 | 105.18 | 105.05 | 104.97 | 104.87 | 104.69 | 104.59 | 104.47 | 104.19 | 104.02 | 103.9

## Slide 9: Modelling
3 data points per bundle are selected (i.e. equally spaced within the bundle constrictions locations).
For each data point (axial location), local temperature and fluence are collected.
In addition the following are collected:
  Relevant manufacturing info
  Relevant channel history (inspection times)
Inspection Data & Independent Variables

## Slide 10: Modelling
Motivation
  Large amount of in-service PTID/WT inspections to date
  Inspection data has consistently shown that design creep rates are conservative
  PT dimensions are highly influential input parameters in FFS assessments
  Support Reactor Life extensions
Statistical Analysis

## Slide 11: Modelling
PTID/WT Model
Model Form - Arrhenius
Θ the operating time in [EFPH (Equivalent Full-Power Hours)],
Ψ is the irradiation fluence in [1023 neutrons/m2],
Ω is a categorical variable for manufacturing process,
K5 is a non-dimensional constant
QIR is the estimated activation energy for irradiation creep K,
Qth is the estimated activation energy for thermal creep K,
ID is the inner diameter in [mm],
T is the operating temperature in [K],
WT is the wall thickness in [mm],
εID and εWT are the random errors associated with the statistical models for the ID and WT
are the model parameters for the ID and WT
Reference: R. A. Holt, “In-reactor deformation of cold-worked Zr-2.5Nb pressure tubes”, Journal of Nuclear Materials, 372 p.182-214, 2008.

## Slide 12: Modelling
Weighted Linear Regression
  Account for multiple inspected PTs
PTID Model
  R2=95.6%
  Standard Error is 0.167 mm (11456 data points)
PTWT Model
  R2=77.4%
  Standard Error is 0.032 mm (11456 data points)
Measurement Resolution=0.01mm for both ID(~105mm) and WT(~4mm)
Model Results for Representative Station

## Slide 13: Modelling
PTID Measured vs. Predicted
Model Results
Chart: Predicted

## Slide 14: Modelling
PTWT Measured vs. Predicted
Model Results
Chart: Predicted

## Slide 15: Uncertainty Characterization
Residual Uncertainty
Compensate for limited coverage
Uncertainty Components – Residual
where, t-dist (ξ) refers to the Student’s t-distribution with ξ degrees of freedom
VID, VWT are the first derivative vectors of the regression function
WID, WWT are the unscaled variance-covariance matrices associated with the regression function accounting for weights

## Slide 16: Uncertainty Characterization
Model Results – ID Profile
Chart: Bundle #
| 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1
2007 Data | 104.54 | 105.66 | 106.24 | 106.33 | 106.18 | 106 | 105.76 | 105.75 | 105.58 | 105.42 | 105.16 | 104.73 | 104.15
Mean Prediction | 104.6586 | 105.6426 | 106.248 | 106.4234 | 106.2949 | 106.0577 | 105.7031 | 105.7097 | 105.5992 | 105.4436 | 105.112 | 104.6506 | 104.0828
97.5% UB | 104.9852 | 105.9691 | 106.5746 | 106.7499 | 106.6214 | 106.3842 | 106.0296 | 106.0362 | 105.9257 | 105.7701 | 105.4384 | 104.9771 | 104.4093
2.5% LB | 104.3321 | 105.3161 | 105.9215 | 106.0968 | 105.9683 | 105.7311 | 105.3766 | 105.3832 | 105.2727 | 105.1171 | 104.7855 | 104.3242 | 103.7563

## Slide 17: Uncertainty Characterization
Model Results – WT Profile
Chart: Bundle #
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13
2010 Data | 4.25 | 4.19 | 4.15 | 4.15 | 4.13 | 4.11 | 4.09 | 4.11 | 4.12 | 4.13 | 4.12 | 4.14 | 4.25
Mean Prediction | 4.2319 | 4.2013 | 4.1747 | 4.1548 | 4.1345 | 4.1126 | 4.101 | 4.0905 | 4.0951 | 4.1063 | 4.1241 | 4.1621 | 4.2149
97.5% UB | 4.2954 | 4.2648 | 4.2382 | 4.2183 | 4.198 | 4.1761 | 4.1645 | 4.1539 | 4.1586 | 4.1698 | 4.1875 | 4.2256 | 4.2784
2.5% LB | 4.1684 | 4.1378 | 4.1112 | 4.0914 | 4.071 | 4.0491 | 4.0375 | 4.027 | 4.0317 | 4.0428 | 4.0606 | 4.0986 | 4.1514

## Slide 18: Uncertainty Characterization
Correlations between uncertainties rather than variables considered
Pair-wise correlation between residual uncertainties in pressure tube inner diameter and wall thickness was characterized
Residual uncertainties and correlations are accounted for in Probabilistic Evaluation
Correlations
Corr(ID,WT) | PTWT Resid
PTID Resid | -0.2389

## Slide 19: Annex G on CSA N285.8
Probabilistic evaluation procedures focussing on uncertainties for influential variables
  Identification of influential variables
  Characterization of uncertainties for influential variables
  Incorporation of uncertainty characterization results into probabilistic evaluation
Uncertainty component on imbalances of model basis data set was not previously characterized
Uncertainty Analysis – Pilot Study

## Slide 20: Uncertainty Characterization
Uncertainty Components
Uncertainty due to model form was not considered
Annex G on CSA N285.8
Variable type | Best estimate obtained using | Uncertainty component | 
Type B | Statistical model |  | Residual uncertainty
 |  |  | Uncertainty due to limitations in model-basis data sets
 |  |  | Uncertainty due to model form

## Slide 21: Annex G – Pilot Study
Uncertainty due to imbalances in model-basis data sets (MBDS)
  Weighted regression on each of the predictor variables
  Operating time Θ: 26 bins for each inspected equivalent full-power hours (EFPH)
  Irradiation fluence Ψ: 21 bins of 100 1023 neutrons/m2
  Operating temperature T: 23 bins of 2 0C
  Manufacturing condition Ω: 2 bins for two conditions (Ω = 1 and Ω = 0)
Repeat multiple weighted regression on the observations and compare to base case residuals
Uncertainty Components

## Slide 22: Annex G – Pilot Study
MBDS imbalances for variable ID
Probability level | Percentile of residuals for weighting case: |  |  |  |  | Uncertainty distribution |  | 
 | Base case | W ¦ T | W ¦ Θ | W ¦Ψ | W ¦ Ω | Lower limit (A) | Upper limit (B) | Range
0.05 | -0.257 | -0.254 | -0.268 | -0.246 | -0.265 | -0.012 | 0.011 | 0.022
0.10 | -0.178 | -0.179 | -0.195 | -0.170 | -0.190 | -0.016 | 0.008 | 0.024
0.15 | -0.131 | -0.131 | -0.147 | -0.127 | -0.143 | -0.016 | 0.005 | 0.021
0.20 | -0.102 | -0.101 | -0.118 | -0.098 | -0.114 | -0.016 | 0.005 | 0.020
0.25 | -0.078 | -0.078 | -0.095 | -0.076 | -0.090 | -0.017 | 0.002 | 0.019
0.30 | -0.058 | -0.058 | -0.075 | -0.057 | -0.070 | -0.017 | 0.001 | 0.018
0.35 | -0.041 | -0.042 | -0.058 | -0.039 | -0.054 | -0.017 | 0.002 | 0.019
0.40 | -0.024 | -0.024 | -0.041 | -0.023 | -0.037 | -0.017 | 0.001 | 0.018
0.45 | -0.008 | -0.009 | -0.025 | -0.007 | -0.021 | -0.017 | 0.000 | 0.018
0.50 | 0.007 | 0.006 | -0.011 | 0.007 | -0.006 | -0.018 | 0.000 | 0.018
0.55 | 0.021 | 0.021 | 0.005 | 0.024 | 0.009 | -0.016 | 0.003 | 0.019
0.60 | 0.038 | 0.037 | 0.021 | 0.039 | 0.025 | -0.017 | 0.002 | 0.019
0.65 | 0.053 | 0.052 | 0.036 | 0.055 | 0.040 | -0.017 | 0.003 | 0.020
0.70 | 0.071 | 0.069 | 0.054 | 0.073 | 0.057 | -0.017 | 0.002 | 0.020
0.75 | 0.091 | 0.090 | 0.074 | 0.095 | 0.078 | -0.017 | 0.003 | 0.021
0.80 | 0.116 | 0.116 | 0.100 | 0.121 | 0.103 | -0.016 | 0.005 | 0.021
0.85 | 0.148 | 0.148 | 0.134 | 0.154 | 0.137 | -0.015 | 0.006 | 0.020
0.90 | 0.193 | 0.192 | 0.177 | 0.200 | 0.180 | -0.016 | 0.008 | 0.023
0.95 | 0.270 | 0.272 | 0.259 | 0.281 | 0.262 | -0.011 | 0.011 | 0.022
Mean estimate |  |  |  |  |  | -0.016 | 0.004 | 0.020

## Slide 23: Annex G – Pilot Study
MBDS imbalances for variable WT
Probability level | Percentile of residuals for weighting case: |  |  |  |  | Uncertainty distribution |  | 
 | Base case | W ¦ T | W ¦ Θ | W ¦Ψ | W ¦ Ω | Lower limit (A) | Upper limit (B) | Range
0.05 | -0.052 | -0.049 | -0.044 | -0.047 | -0.048 | 0.003 | 0.008 | 0.005
0.10 | -0.043 | -0.040 | -0.035 | -0.038 | -0.039 | 0.003 | 0.008 | 0.005
0.15 | -0.037 | -0.034 | -0.029 | -0.032 | -0.033 | 0.003 | 0.008 | 0.005
0.20 | -0.032 | -0.029 | -0.024 | -0.027 | -0.028 | 0.003 | 0.008 | 0.005
0.25 | -0.027 | -0.024 | -0.019 | -0.023 | -0.023 | 0.003 | 0.008 | 0.005
0.30 | -0.023 | -0.021 | -0.015 | -0.019 | -0.020 | 0.003 | 0.008 | 0.005
0.35 | -0.019 | -0.017 | -0.012 | -0.015 | -0.016 | 0.003 | 0.008 | 0.005
0.40 | -0.015 | -0.013 | -0.008 | -0.011 | -0.012 | 0.003 | 0.008 | 0.005
0.45 | -0.011 | -0.009 | -0.004 | -0.007 | -0.008 | 0.003 | 0.007 | 0.005
0.50 | -0.007 | -0.004 | 0.001 | -0.003 | -0.003 | 0.002 | 0.007 | 0.005
0.55 | -0.002 | 0.000 | 0.005 | 0.001 | 0.001 | 0.003 | 0.007 | 0.005
0.60 | 0.003 | 0.005 | 0.010 | 0.007 | 0.006 | 0.003 | 0.008 | 0.005
0.65 | 0.007 | 0.010 | 0.015 | 0.011 | 0.011 | 0.003 | 0.008 | 0.005
0.70 | 0.012 | 0.015 | 0.020 | 0.016 | 0.016 | 0.003 | 0.008 | 0.005
0.75 | 0.018 | 0.021 | 0.026 | 0.022 | 0.022 | 0.003 | 0.008 | 0.005
0.80 | 0.024 | 0.026 | 0.032 | 0.028 | 0.027 | 0.002 | 0.008 | 0.005
0.85 | 0.031 | 0.034 | 0.039 | 0.036 | 0.035 | 0.003 | 0.008 | 0.005
0.90 | 0.040 | 0.043 | 0.048 | 0.044 | 0.044 | 0.003 | 0.008 | 0.005
0.95 | 0.053 | 0.055 | 0.061 | 0.058 | 0.056 | 0.003 | 0.008 | 0.006
Mean estimate |  |  |  |  |  | 0.003 | 0.008 | 0.005

## Slide 24: Annex G – Pilot Study
For the variables ID and WT
Uniform (A, B) refers to the uniform distribution between lower limit A and upper limit B
Uncertainty due to imbalances in the model basis data set is smaller than the residual uncertainty and therefore there is no issue due to imbalance of the data sets
Uncertainty Components
Variable | Residual uncertainty | Uncertainty due to imbalances in model-basis data set
Pressure tube inner diameter | SID = 0.167 [mm], ξID = 11452 | Uniform (−0.016, 0.004) [mm]
Pressure tube wall thickness | SWT = 0.032 [mm], ξWT = 11452 | Uniform (0.003, 0.008) [mm]

## Slide 25: Conclusions
Pressure Tube ID and WT models based on in-service inspection data have been developed.
Correlation between the residual uncertainties of the two models was determined.
During a pilot study on uncertainty analysis, the uncertainty due to imbalances in the model basis dataset was characterized for these two models.
  For both models, it was concluded that the uncertainty due to imbalances in the MBDS was significantly smaller than the residual uncertainty.

## Slide 26: Acknowledgements
Kinectrics
Bruce Power
Ontario Power Generation
CANDU Owners Group