## Slide 1
Monte Carlo Defect Tolerance Assessment of a Plant Weld for Increased Life
ISPMNA 2022
Ben Pellereau, Technical Specialist
November 2022
© 2022 Rolls-Royce plc The information in this document is the property of Rolls-Royce plc and may not be copied or communicated to a third party, or used for any purpose other than that for which it is supplied without the express written consent of Rolls-Royce plc.
This information is given in good faith based upon the latest information available to Rolls-Royce plc, no warranty or representation is given concerning such information, which must not be taken as establishing any contractual or other commitment binding upon Rolls-Royce plc or any of its subsidiary or associated companies.

## Slide 2
Background
01

## Slide 3: Description of Component
Multi-stage weld between a forging and a tube:
  Weld buttering deposited on tube OD and weld prep
  PWHT carried out on buttering
  Tube inserted through forging
  Weld completed (no PWHT)
Assessment was part of consideration of re-using old part
New part would have no crevice and full PWHT, but manufacturing could take longer than refurbishment
Background
Ferritic forging/tube
Buttering
Weld
Crevice

## Slide 4: Historic Justification
Postulated defects in multiple locations
  Corner (rad-axi)
  Weld defect and weld/buttering interface (rad-axi, axi-circ)
  Buttering/forging interface (rad-axi, axi-circ)
  Main forging (rad-axi)
Deterministic assessment against target RFK (1 or 1.4)
Supporting probabilisitic assessments for low RFK
  Weld and interface positions
Background
Probabilistic assessment region

## Slide 5
Probabilistic Assessment
02

## Slide 6
Chart: 
| 45 | 70 | 100 | 150 | 200 | 250
Series 1 | 11.1 | 23.6 | 178.5 | 194.4 | 163 | 51.3
Probabilistic Assessment Overview
Define initial defect
Sample depth and position
Sample ligament size
‘Snap through’ (ductile or brittle approach)
Sample material properties
WRS (normal dist. of σy)
Calculate end of life SIF
Identify outcome
Determine crack front length
Defect present in weld and/or buttering?
Crack growth rate
Toughness – temperature dependent (master curve transition and upper shelf)
Combine pressure, fit-up, thermal and WRS
R6 FAD-based KI to KJ
Simple SIF, KI = Yσ√[πa]
Compare KJ with Kc & Kd
Report result
Sum failures and divide by number of simulations
Factor to define primary / secondary interaction
Distribution on Kd
Distribution on T0
σth
temp
Kc < KJ < Kd → cleavage failure, no tearing
Kd < Kc < KJ → cleavage after tearing
Kd < KJ < Kc → tearing, no cleavage
Otherwise, no failure

## Slide 7: Defect Distribution
75% chance of defect in weld
12.5% chance of defect in buttering
Size from 2 parameter Weibel distribution with maximum
Defined based on expert elicitation
Benchmark against defects in deterministic assessment:
Uniform distribution for ligament: 0 to 20% of crack depth
Assessment Overview
Cut-off @ 5mm
PDF of defect size

## Slide 8
Initial Results
03

## Slide 9
Crack Growth Fitting - Original
4 orders of magnitude
Why so different?

## Slide 10: Crack Growth Fitting - Original
Deterministic growth law:
Assume that K is proportional to √a
Re-format FCG law as:
Use deterministic growth calcs using mean and 95% bound to determine mean and standard deviation of E (log-normal)
Log mean varied with location, log sd assumed constant
E only obtained for rad-axi defects, assumed same for axi-circ
Initial Results

## Slide 11: Crack Growth Fitting – New Assessment
Initially same approach taken
Growth rate 2.2-3.5x faster
  ~2x the number of transients
  Growing into region where growth rate ramps up
Defects chosen for FCG calc not necessarily typical of those that caused failures
FCG relationship therefore overly conservative for many of the sampled defects
Initial Results
Additional life
Original life

## Slide 12: Impact on Results
Initial Results
acceptable defect size
Previous assessment:
Defects close to failing, but this wasn’t known due to binary output
New assessment:
Extra growth tips edge cases into failure
Reduction in Kmat due to ageing
initial defect sizes
Increased growth results in many more cases failing, even with smaller defects
final defect size

## Slide 13
Revised Assessment
04

## Slide 14: Crack Growth Fitting – New Assessment
For project timescale needed a “simple” but powerful fix!
Additional parameter added – E refitted as a function of ainitial
E values obtained for both defect orientations
Range of defect sizes used (previously just 1)
Revised Assessment
Location | Radial-axial | Axial-circ
Tube interface | E ~constant | E increases with a
Forging interface | E decreases with a | E decreases with a

## Slide 15
Revised Assessment
Difference between green/orange and blue/red lines shows conservatism in previous approach – noting log scale
Couple of examples of the results shown

## Slide 16
Crack Growth Fitting - Original

## Slide 17
Conclusions
05

## Slide 18: Key Lessons Learned
Simplified models are often needed in probabilistic assessments
However:
Small changes to inputs may invalidate associated assumptions
In models with binary output, cliff edges are hard to predict
Sensitivity studies are key to confirming model suitability
Conclusions

## Slide 19
Copy here